Section 09 6813 
Tile Carpeting

  - ************************************************************************************************************

    - LANL MASTER SPECIFICATION SECTION

Rev. 4 Summary of Changes: Edited and updated as required for import into SpecLink.

      - NOTE TO SPECIFIER ON USAGE IN SPECLINK: Activate the Section by turning on Seq #0000, followed by activating paragraphs in PART 1, Article SECTION INCLUDES. This will activate related articles, paras/subparas in the rest of the Section (i.e., SECTION INCLUDES in PART 1 activates articles and paras/subparas in PARTS 2 and 3). If there are choice fields to edit the entire Section (typically in this first author note or beginning of the Section), make selections at those locations, which will filter through the remaining Section. All Articles, paragraphs and subparagraphs must be activated sequentially from top to bottom, unless noted otherwise.

      - This template must be edited for each project. In doing so, Specifier must add job-specific requirements. Selections and choice fields are used to indicate designer choices or locations where text must be supplied by the designer. The section must also be edited to remove requirements for processes, items, or designs that are not included in the project.

      - To seek a variance from applicable requirements in this Section, contact the Engineering Standards Manual (ESM) Architectural POC  (LANL access only). Please contact POC with suggestions for improvement as well. LANL personnel should submit here: Suggested Change or Request Clarification; subcontractors via email to engstandards@lanl.gov.

      - When assembling a specification package, include applicable Sections from all Divisions, especially Division 1, General Requirements.

      - Section is developed for ML-4 projects.  For ML-1, 2, and 3 applications, additional requirements and independent reviews should be added if increased confidence in procurement or execution is desired; see LANL ESM Chapter 1 - General, Section Z10 Specifications and Quality sections.

  - ************************************************************************************************************

PART 1 - GENERAL

SECTION INCLUDES

Carpet tiles with ​​​<< Click to select the installation method from the drop down menu;  Glue-down installation;  Self-adhesive installation; or  Glue-down and Self-adhesive installation>>​​​.

Accessories.

RELATED REQUIREMENTS

Section << 01 2500 - Substitution Procedures>>

Section << 01 8113.13 - Sustainable Design>>

REFERENCE STANDARDS

16 CFR 1630 - Standard for the Surface Flammability of Carpets and Rugs (FF 1-70).

AATCC Test Method 20 - Test Method for Fiber Analysis: Qualitative.

AATCC Test Method 134 - Test Method for Electrostatic Propensity of Carpets.

AATCC Test Method 165 - Test Method for Colorfastness to Crocking: Textile Floor Coverings - Crockmeter.

AATCC Test Method 189 - Test Method for Fluorine Content of Carpet Fibers.

AATCC TM16.3 - Test Method for Colorfastness to Light:  Xenon-Arc.

ABA Standards - ABA Accessibility Standards.

ASTM D1335 - Standard Test Method for Tuft Bind of Pile Yarn Floor Coverings.

ASTM D2859 - Standard Test Method for Ignition Characteristics of Finished Textile Floor Covering Materials.

ASTM D3676 - Standard Specification for Rubber Cellular Cushion Used for Carpet or Rug Underlay.

ASTM D3936 - Standard Test Method For Resistance To Delamination Of The Secondary Backing Of Pile Yarn Floor Covering.

ASTM D5116 - Standard Guide for Small-Scale Environmental Chamber Determinations of Organic Emissions from Indoor Materials/Products.

ASTM D5252 - Standard Practice for the Operation of the Hexapod Tumble Drum Tester.

ASTM D5417 - Standard Practice for Operation of the Vettermann Drum Tester.

ASTM E648 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

ASTM E662 - Standard Test Method for Specific Optical Density of Smoke Generated by Solid Materials.

CRI (GL) - Green Label Testing Program - Certified Products.

CRI (GLP) - Green Label Plus Testing Program - Certified Products.

CRI 104 - Standard for Installation of Commercial Carpet.

CRI Test Method 101 - Assessment of Carpet Surface Appearance Change using the CRI Reference Scales.

IES TM-30 - Technical Memorandum: IES Method for Evaluating Light Source Color Rendition.

ISO 2551 - Textile Floor Coverings and Textile Floor Coverings in Tile Form - Determination of Dimensional Changes Due to the Effects of Varied Water and Heat Conditions and Distortion Out of Plane.

NFPA 101 - Life Safety Code.

NFPA 253 - Standard Method of Test for Critical Radiant Flux of Floor Covering Systems Using a Radiant Heat Energy Source.

TTPIA - 15 USC 70, The Textile Products Identification Act.

      - ***************************************************************************************

      - Edit submittals to include only those absolutely necessary to assure the requirements and features that are important for the specific project will be met.

      - ***************************************************************************************

SUBMITTALS

Action Submittals:

Catalog data on carpet tiles, describing physical<< and performance; or  None - N/A>> characteristics; sizes, patterns,<< colors available,; or  None - N/A>> and method of installation.

Manufacturer's certificate indicating that products meet or exceed the specified requirements and tests per Article << 2.3; or  _______>> Performance Requirements.

        - ******************************************************************************

        - Retain the following subparagraph when project requires samples.

        - ******************************************************************************

Samples: Four carpet tiles illustrating proposed color<< and pattern design; or  None - N/A>> for each carpet selected.

Shop drawings indicating layout of joints, direction of carpet weave and cut tiles.

        - ******************************************************************************

        - Verify these requirements below against LANL ESM Chapter 14 - Sustainable Design, Attachment 1 "Required Attribute" Column and, if applicable, the LEED prerequisites and project credits. Material content and BioPreferred/recycled content required. The remaining submittals are designer-choices based on project-specific requirements. This subparagraph with subparagraphs below it are activated automatically based on selections made in Article Performance Requirements in PART 2, when applicable.

        - ******************************************************************************

Sustainable Design Submittals:

Sustainable Design (SD) Submittals: Provide material content documentation in accordance with the requirements of this Section. ​​​​​​​​​​​​​<< Submit any additional documentation for this product category, as applicable under Section  01 8113.13 - Sustainable Design , with this Section’s submittal.; or  None - N/A>>​​​​​​​​​​​​​

Submit manufacturer’s documentation of Biopreferred/recycled content for each product.

          - **********************************************************************

          - The following subparagraph is a designer-choice. Retain when required for project.

          - **********************************************************************

Submit manufacturer’s documentation that carpet, cushion and adhesives meet the Sustainable Design requirements (Green Label Plus and Green Label certificates and VOC limits) per Article ​​<< 2.3; or  _______>>​​ Performance Requirements.

Informational Submittals:

Manufacturer’s installation instructions indicating procedures for installing carpet products and accessories.

At Closeout:

Maintenance Instructions: Submit manufacturer’s printed instructions for maintenance of installed work, including methods and frequency recommended for maintaining optimum condition under anticipated traffic and use conditions. Include precautions against materials and methods which may be detrimental to finishes and performance.

Warranty.

      - ***************************************************************************************

      - Retain the following Article Extra Materials when required for project.

      - ***************************************************************************************

EXTRA MATERIALS

Provide << 5 percent; or  _______>> of required quantity of carpet tiles of each color selected in their original containers.

QUALITY ASSURANCE

Manufacturer Qualifications: Firm with not less than 5 years of production experience, whose published literature clearly indicates general compliance of products with requirements of this Section.

Installer Qualifications: Firm with not less than 5 years of experience in installation of commercial carpet tile of type, quantity and installation methods similar to work of this Section. Installer shall be approved by manufacturer.

Labeling: A label meeting the Federal Labeling Requirements, as stated in Federal Trade Commission's <<TTPIA>>, shall be attached to the certification samples and the products delivered.

Carpet covered by this Section is intended for end use applications that have a Severe Use Classification. It is the Subcontractor’s responsibility to provide only products compatible with adjacent materials in the assembly.

Carpet tiles shall be installed using manufacturer’s recommended adhesive system. A combination of factory-applied self-adhesive tiles and field-applied pressure-sensitive adhesive may be used, provided all materials are from the same manufacturer and meet performance requirements for the intended space.

All products within the same floor of a project shall be from the same dye lot.

Patterns and colorways shall be available for a minimum of ten (10) years.

      - ***************************************************************************************

      - Retain the following Article Mockup only when required for project.

      - ***************************************************************************************

MOCKUP

Provide mockup for approval by LANL of special cuts/effects such as mitered corners at borders or graphic patterns that are prepared and installed onsite.

DELIVERY, STORAGE, AND HANDLING

Comply with <<CRI 104>>, Section 4.0, “Storage and Handling”.

Prior to installation, store materials for three (3) days in area of installation to achieve temperature stability.

Maintain minimum 70 degrees F ambient temperature three days prior to, during, and 24 hours after installation of materials. In addition, maintain the relative humidity at approximate level at which the area is to be maintained.

WARRANTY

Provide written warranty for all labor and materials, signed by Subcontractor, Installer, and Manufacturer agreeing to repair or replace defective materials and workmanship of carpet installation during a << 2; or  _______>> year period following final acceptance.

Provide non-prorated 15 year warranty against wear and lifetime warranty against loss of anti-static properties, from date of substantial completion.

PART 2 - PRODUCTS

    - **********************************************************************************************

      - The following Article Product Options and Substitutions is a designer-choice Retain when project allows for substitutions.

    - **********************************************************************************************

PRODUCT OPTIONS AND SUBSTITUTIONS

Alternate products may be accepted; follow Section << 01 2500 - Substitution Procedures>>.

MANUFACTURERS

Interface Company

Mannington Mills Inc.

Milliken Contract Carpets

Mohawk Group

Shaw Contract Group

<< _______>>

PERFORMANCE REQUIREMENTS

Compatibility: Provide carpet, adhesives, and other related materials that are compatible with one another and with substrates under conditions of service and application.

Physical Performance Requirements:

Appearance Retention Rating: Severe (short-term not less than 4.0, long-term not less than 3.5) based on <<ASTM D5252>> (Hexapod) using 3750-gram tumbler or <<ASTM D5417>> (Vettermann) test method. Carpets shall be tested without underlay. The exposure conditioned carpet shall be assessed according to  <<CRI Test Method 101>> and <<IES TM-30>>.

Tuff Bind: Minimum Average value 8.0 pounds (Loop Pile).

Dimensional Stability: Maximum dimensional change plus or minus 0.2 percent.

Delamination Resistance of the Secondary Backing: Not less than 2.5 pounds per inch.

Colorfastness (entire color line):

To Crocking: Color transfer Class 4 minimum, wet and dry, when tested as specified.

To Light: Color contrast between the exposed and unexposed carpet areas equivalent to a minimum of Grade 4 on the Gray Scale for Color Change after an exposure to 60 AFU (AATCC fading units) for all colors.

Fluorochemical Finish: Minimum average of 350 parts-per-million fluorine on the pile fiber when tested in accordance with <<AATCC Test Method 189>>.

Antimicrobial Activity: Inherently antimicrobial, topical finishes not allowed.

Electrostatic Propensity: Maximum 3.5 kV.

Flammability:

Methenamine Pill Test:  Self Extinguishing – compliance with <<16 CFR 1630>> when tested in accordance with <<ASTM D2859>>.

Radiant Panel: Carpets and rugs shall have a critical radiant flux not less than the following: 0.45 W/sq cm in areas unprotected by an automatic fire suppression system and 0.22 W/sq cm in areas protected by an automatic fire suppression system.

Smoke Density: Maximum 450.

Material and Construction Requirements: Carpet tile shall conform to the following criteria:

Pile Fiber Type: 100 percent continuous filament nylon, Type 6 or Type 6.6.

Backing Materials:

Primary Backing: 100 percent synthetic materials.

Secondary Backing: Fiberglass reinforced secondary backing consisting of a polymeric cushion or hard back compound consistent with all performance testing requirements.

Surface Texture: Level or textured loop, multi-level loop, or pattern.

Yarn: Multi-ply.

Tufting Machine Gauge: Minimum << 1/10; or  _______>> inch.

Number of Stitches: Minimum << 8; or  _______>> per inch.

Pile Height: ​<< 0.125 to 0.5; or  _______>>​ inch.

Face/Pile Weight: Minimum << 20; or  _______>> oz/sq yd.

Dye Method: Yarn or solution dyed.

Color and Pattern: Selected by the Architect and approved by LANL from Manufacturer's color line of product meeting this Section.

Product shall have a lead time of not more than six (6) weeks from the time the Supplier receives the order to the time LANL receives the product.

Sustainable Design Requirements:

BioPreferred/Recycled Content:

Nylon Carpet Face Fiber: BioPreferred. Minimum 7 percent biobased content.

Nylon Carpet Backing: For vinyl primary backing, use the highest percentage of total recovered materials content available; however, 0 percent is not acceptable.

Synthetic Fibers Carpet Cushion: 100 percent recovered carpet fabrication scrap.

        - ******************************************************************************

        - The following subparagraph is a designer-choice. Retain when required for project.

        - ******************************************************************************

Indoor Air Quality:

Carpet: Shall be only those certified with <<CRI (GLP)>>.

Cushion: Shall be only those certified with <<CRI (GL)>>.

Adhesive: VOC level shall not exceed 50 g/L.

Accessibility Requirements:

Carpet pile, transitions and floor slopes must comply with <<ABA Standards>>​.

ACCESSORIES

Floor Patching/Leveling Compound: << White premix latex; or  _______>>; type recommended by carpet manufacturer for specific substrate material.

Releasable Adhesive for Carpet: Provide water resistant, low VOC, non-staining type as recommended by carpet manufacturer which complies with flame spread rating required for carpet installation.

      - ***************************************************************************************

      - Retain the following paragraph when concrete floor is present on project.

      - ***************************************************************************************

Concrete Sealer: Provide concrete sealer compatible with carpet backing material and adhesive.

      - ***************************************************************************************

      - The following two paragraphs are designer-choices for edge guard type. Metallic edge guards are used in high-traffic or commercial areas where durability, impact resistance, and longevity are priorities - for example, at door thresholds, elevator lobbies, or transition zones between carpet and hard surfaces. Non-metallic edge guards are often used in office interiors, or areas of lower foot traffic where flexibility, cost efficiency, and aesthetics blending with flooring are more important.

      - ***************************************************************************************

Carpet Edge Guard, Metallic: Extruded aluminum bend-down type edge guard with concealed gripper teeth and minimum 1-1/2 inch wide anchorage flange and minimum 5/8 inch wide face flange. Provide with anodized aluminum finish of colors, selected by LANL, from manufacturer's standard available colors.

Carpet Edge Guard, Non-metallic: Extruded or molded heavy-duty vinyl or rubber carpet edge guard of size and profile indicated, with a minimum 2 inch wide anchorage flange; colors selected by LANL from manufacturer's standard available colors.

Vinyl Base: 4 inches high, coved, 0.080 inch gauge.

Miscellaneous Materials: As recommended by manufacturer of carpet and other carpeting products for intended application.

SOURCE QUALITY CONTROL

Flammability Tests:

Radiant Panel: <<ASTM E648>>, Class I.

Smoke Density: <<ASTM E662>>.

Methenamine Pill Test: Self Extinguishing (<<16 CFR 1630>> or <<ASTM D2859>>).

Lightfastness: <<AATCC TM16.3>>.

Crocking: <<AATCC Test Method 165>>.

Static Electricity:  <<AATCC Test Method 134>>.

Dimensional Stability: <<ISO 2551>>.

Turf Bind: <<ASTM D1335>>.

Delamination Resistance: <<ASTM D3936>>.

Fluorochemical Finish: <<AATCC Test Method 189>>.

Electrostatic Propensity:  <<AATCC Test Method 134>>.

Indoor Air Quality: <<ASTM D5116>>.

Pile Fiber Identity: <<AATCC Test Method 20>>.

Backing Material Identity: <<AATCC Test Method 20>>.

Attached Backing:

Thickness: <<ASTM D3676>>.

Volume Density: <<ASTM D3676>>.

Compression Resistance: <<ASTM D3676>>.

Compression Set: <<ASTM D3676>>.

Test in accordance with <<NFPA 253>> (<<ASTM E648>>) when applying the floor finish requirements of <<NFPA 101>> to DOE Facilities.

PART 3 - EXECUTION

    - **********************************************************************************************

      - Retain the following Article Carpet Removal  if project involves removal of existing carpet.

    - **********************************************************************************************

CARPET REMOVAL

All carpet tile and scraps removed from LANL projects shall be recycled or reapplied. Disposal of product in landfill is not permitted.

Vacuum in-place carpet with industrial vacuum prior to demolition or debris-producing renovation.

Remove carpet.

Stack on pallets for handling.

Store carpet off ground and under cover to prevent contamination of materials by water, foreign matter, or other causes.

Coordinate with manufacturer for pickup for recycle. In the case that the manufacturer does not have a recycling program, contact an independent recycling program.

EXAMINATION

Examine substrates for moisture content, alkaline presence and other conditions on which carpet tile is to be installed.

Provide Calcium Chloride test results to verify amount of moisture in new or existing slabs.

Calcium Chloride shall be less than or equal to three (3) pounds per one thousand (1000) square feet in 24 hours.

Alkalinity testing shall result in a pH range of 5-9.

Notify LANL in writing of conditions detrimental to proper completion of the work.

Do not proceed until unsatisfactory conditions have been corrected.

Field-verify all dimensions and other work conditions affecting the installation of carpet tile.

Verify that substrate surfaces are smooth and flat with maximum variation of 1/8 inch in 10 feet and are ready to receive work before beginning installation.

PREPARATION

General: Comply with <<CRI 104>>, Section 7.0, “Site Conditions" and Section 8.0, "Substrate Preparation,” and carpet tile manufacturer’s written installation instructions for preparing substrates indicated to receive carpet tile installation.

        - ******************************************************************************

        - Retain the following subparagraph when concrete floor is present on project.

        - ******************************************************************************

Concrete shall be cured, clean and dry before installation proceeds.

Repair minor holes, cracks, depressions, or rough areas using floor patching/leveling compound that is compatible with the adhesive to be used. Protrusions over 1/32 inch shall be leveled. Large, patched areas shall be primed.

Whenever a powdery or porous surface is encountered, a primer compatible with the adhesive shall be used to provide a suitable surface for glue-down installation.

        - ******************************************************************************

        - The following subparagraph is a designer-choice. Retain based on project-specific conditions.

        - ******************************************************************************

Remove existing utility caps and install grout fill caps; grout level with existing substrate.

Remove grease, oils, loose particles, paint, dirt, curing and parting agents, and all foreign substances. Clear away debris and scrape up cementitious deposits from surfaces to receive carpet tile; vacuum clean immediately before installation.

Subfloor shall be level and smooth and free from scaling and irregularities per <<CRI 104>>.

Coordinate carpet installation with any underfloor electrical/telephone/data for conductors and cables to be pulled prior to carpet installation.

Accessories shall be installed on top of carpet after installation.

Sequence carpet tile installation with other work to minimize possibility of damage and soiling of carpet during remainder of construction period.

      - ***************************************************************************************

      - The following four paragraphs are designer-choice. Retain the first or second paragraph when concrete floor is present on project based on project-specific conditions. Retain the third paragraph when wood floor is present on project. Retain the fourth paragraph when vinyl tile is present on project and requires replacement.

      - ***************************************************************************************

Concrete (No Previous Flooring Material): Apply a concrete sealer coat at the rate recommended by the sealer manufacturer. Use thin, fast drying primers that are compatible with adhesives. Apply adhesive only after primer is completely dry.

Concrete (Previous Flooring Material): Remove existing adhesive by grinding with a concrete grinding machine and moist sand. Do not use solvents to remove adhesive. Apply concrete sealer at rate recommended by sealer manufacturer. Use thin, fast drying primers that are compatible with adhesives. Completely cover area with cutback neutralizer per manufacturer’s recommendation.

Wood: Patch all surface irregularities and seal with wood sealer as recommended by manufacturer.

Vinyl Tile: Replace all loose, missing, and broken tiles with tiles of equal thickness making note of any special requirements with respect to asbestos. Strip existing tile of wax, dirt and other foreign substances. Completely cover area with cutback neutralizer per manufacturer’s recommendations.

Proceed with installation only after unsatisfactory conditions have been corrected.

INSTALLATION

General:  Comply with <<CRI 104>>, Section 10.0, “Carpet Tile Installation", and carpet tile manufacturer’s written instructions, except where more stringent requirements are shown or specified, and except where project conditions require extra precautions or provisions to ensure satisfactory performance of the Work.

Unless otherwise noted or approved on drawings, begin laying tile at the centerline of the area or room.

Comply with carpet tile installation instructions for direction of carpet tile. Unless otherwise noted on drawings, align pattern and pile in the same direction, parallel to the centerline of the area or room.

Extend carpet tile under open-bottom obstructions and under removable flanges and furnishings, and into alcoves and closets of each space.

          - **********************************************************************

          - The following subparagraph is a designer-choice. Retain based on project-specific conditions.

          - **********************************************************************

Existing systems furniture shall be raised or removed to accommodate continuous carpet installation.

Provide cut-outs where required, and bind cut edges where not concealed by protective edge guards or overlapping flanges.

        - ******************************************************************************

        - Retain the following subparagraph when carpet edge guard required for project.

        - ******************************************************************************

Install carpet edge guard where edge of carpet is exposed; anchor guards to substrate. Use full-length strips only.

Expansion Joints: Do not bridge building expansion joints with carpet tile; provide for movement.

Carpet tile shall be free from movement when subjected to traffic.

Do not use pieces smaller than 1/3 of a standard tile without prior approval by LANL.

At floor finish material changes at doors, place centerline of abutting materials below door.

      - ***************************************************************************************

      - The following three paragraphs are designer-choice. Retain paragraphs based on installation method selected for project.

      - ***************************************************************************************

Glue-Down Installation

Fit sections of carpet tile into each space prior to application of adhesive. Trim edges.

Apply a full spread of adhesive uniformly to substrate in accordance with manufacturer’s instructions unless otherwise indicated by LANL.

Follow MSDS instructions for ventilation requirements.

Butt carpet tile edges tightly together to form seams without gaps. Butt edges tightly to vertical surfaces.

Eliminate air pockets and ensure uniform bond.

Remove adhesive promptly from face of carpet tiles.

Self-Adhesive Installation: Install per manufacturer’s recommendation.

Miscellaneous Installation, Stairway Carpeting: Install per manufacturer’s recommendation. Provide vinyl nosing at each riser. Match adjoining carpet installation.

Install vinyl base after completion of carpet work. Use adhesive recommended by vinyl base manufacturer.

Coordinate adhesive blocking areas with LANL when floating carpet tile over access flooring.

CLEANING AND PROTECTION

Remove and dispose of debris and recycle all unusable scraps.

Remove excess adhesive and other surface blemishes using cleaner recommended by carpet tile manufacture. Replace carpet tile where blemishes cannot be removed. Trim protruding face yarn from carpet tile surface. Vacuum carpet tile using commercial quality vacuum cleaner with face-beater element.

Protect installed carpet tile to comply with <<CRI 104>>, Section 11.0, “Post Installation”.

Prohibit traffic from carpet areas for 24 hours after installation.

Protect installed carpet with a heavy, non-staining building paper. Do not use a moisture barrier such as plastic film. Maintain protection intact until final acceptance by LANL.

Advise LANL of protection methods and materials necessary to prevent deterioration or damage until substantial completion.

END OF SECTION

    - **********************************************************************************************

      - Do not omit the following reference information:

    - **********************************************************************************************

THE FOLLOWING STATEMENT IS FOR LANL USE ONLY

THIS PROJECT SPECIFICATION SECTION IS BASED ON LANL MASTER SPECIFICATION SECTION 09 6813, REV. 4, DATED APRIL 15, 2026.